## Slide 1
Metal hydride nanocomposites as transition metal free catalysts for ammonia synthesis
Juliette Verschoor, MSc
Materials Chemistry and Catalysis, Debye Institute for Nanomaterials Science, Utrecht University.
18th International Symposium on Metal Hydride Systems, May 2024

## Slide 2
Ammonia as an energy carrier
High energy density (17.7 wt.% H)
Haber-Bosch process
Ease of storage
Provide H2
Ammonia is increasingly recognized as a highly viable chemical energy carrier.
Züttel et al., Phil. Trans. R. Soc. A, 2010, 368, 3329
Schüth et al., Energy Environ. Sci., 2012, 5, 6278
NH3
Volume based
Weight based

## Slide 3
N2 + 3H2 2NH3 ∆H°= -92 kJ mol-1 ∆S°= -198 J k-1 mol-1
For high ammonia yield: low temperature and high pressure
(from thermodynamics)
For fast ammonia formation: high temperature
(from kinetics)
Efficient ammonia production
Reaction at temperatures as low as possible
Ammonia synthesis
Catalysts

## Slide 4
Alkali hydride mediated ammonia synthesis
Wang, Peikun, et al. Nature chemistry 9.1 (2017): 64-70.
Chang, Fei, et al. Nature Catalysis 5.3 (2022): 222-230.
3d TM+LiH composite catalysts achieved ammonia synthesis at a temperatures as low as 150C
KHC nanocomposites catalysts achieved ammonia synthesis at temperatures as low as 250C
NH3 synthesis catalyzed by different catalysts under the conditions of 1 MPa, 1N2:3H2 and flow rate = 60,000 (left) – 36,000 (right) mL gcat-1 h-1.

## Slide 5
Alkali hydride mediated ammonia synthesis
Chang, Fei, et al. Nature Catalysis 5.3 (2022): 222-230.
Are other alkali metal (hydride) carbide nanocomposites also active for ammonia synthesis?
How does the synthesis method affect the activity?

## Slide 6
Alkali hydride carbide: melt infiltration
K+
H-
KH/C
Turbostratic graphite (C) +
Potassium hydride (KH)
Melt infiltration
(200°C, Ar, 10h)
Intercalation
(400°C, Ar, 2h)
KHxCy
Chang, Fei, et al. Nature Catalysis 5.3 (2022): 222-230.

## Slide 7
Besides KH, NaH & LiH based catalysts are also active towards ammonia synthesis
AH-Carbon for ammonia synthesis
NH3 synthesis catalyzed by different catalysts under the conditions of 1 MPa, 300-400 ℃, 1N2-3H2 and flow rate = 60,000 mL gcat-1 h-1.

## Slide 8
Intercalation might not be required for ammonia synthesis activity.
AH-Carbon for ammonia synthesis
NH3 synthesis catalyzed by different catalysts under the conditions of 1 MPa, 300-400 ℃, 1N2-3H2 and flow rate = 60,000 mL gcat-1 h-1.

## Slide 9
Alkali hydride carbide: ball milling
K+
H-
KH/C
Turbostratic graphite (C) +
Potassium hydride (KH)
Heat treatment
(400°C, Ar, 2h)
KHxCy
Ball Milling
500rpm, 6h, 20:1

## Slide 10
KH-C: BM effect on 20wt%KH
NH3 synthesis catalyzed by different catalysts under the conditions of 1 MPa, 300-400 ℃, 1N2-3H2 and flow rate = 60,000 mL gcat-1 h-1.
BM can be used to synthesize KHC ammonia catalyst, but prone to destruction

## Slide 11
NaH-C: BM effect on 10wt%NaH
BM can be used to synthesize NaH/C ammonia catalyst, less prone to destruction in contrast to KHC

## Slide 12
AH-C: ball mill vs melt infiltration
NH3 synthesis catalyzed by different catalysts under the conditions of 1 MPa, 300-400 ℃, 1N2-3H2 and flow rate = 60,000 mL gcat-1 h-1.

## Slide 13
Conclusion
In addition to KH, NaH and LiH based catalysts are also active towards ammonia synthesis.
Both ball milling and melt infiltration are suitable synthesis methods for the synthesis of alkali hydride-based ammonia catalysts from alkali hydrides and graphitic carbon materials.
Intercalation might not be required for ammonia synthesis activity.

## Slide 14
Acknowledgement
Peter Ngene & Petra de Jongh
Jan Willem de Rijk
All of MCC
European Union – AMBHER consortium
Thank you for you attention
Ammonia and MOF Based Hydrogen storagE for euRope