## Slide 1
N
H
H
H
Experimental investigation of carbon membrane for NH3 separation
I. Gargiulo1, D.A. Pacheco Tanaka2, M. A. Llosa Tanco2, F. Gallucci1
Sustainable Process Engineering – Chemical Engineering and Chemistry – Eindhoven University of Technology
TECNALIA, Energy and Environment Division, Mikeletegi Pasealekua 2, 20009 San Sebastian-Donostia, Spain
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)

## Slide 2
N
H
H
H
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
NH3 as long-term hydrogen storage
Renewable
energy
Ammonia
synthesis
Ammonia transport
and storage
Ammonia
decomposition
Ammonia direct
utilization
Hydrogen
utilization
NH3
H2
N2
2

## Slide 3
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
AMBHER target
Catalytic membrane reactor
for in-situ removal of NH3
Shifting the thermodynamic equilibrium
Effective heat management
Energy efficiency
Process intensification
Process conditions:
T=400-500 °C
P=100-200 bar
Target conditions:
T=250-300 °C
P=20 bar
Shifting the equilibrium towards products
(Le Chatelier’s principle)

## Slide 4
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Membrane selection
Carbon membrane
Tailored Pore Structure
High thermal- chemical stability
Surface Functionalization
Ceramic support
Carbonized polymer layer
Molecular sieving (dp<0.2 nm)
Adsorption diffusion (dp<2 nm)
Kinetic diameter
N2>H2>NH3
0.364>0.289>0.26 nm
Surface affinity with gases
Arrhenius equation

## Slide 5
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Membrane characteristic investigation
Molecular sieving
Adsorption diffusion
Kinetic diameter
N2>H2>NH3
3.64>2.89>2.6 nm
Surface affinity with gases
Carbonization temperature tuning
Functionalization of the polymer
PARAMETERS INVESTIGATION
M+
Metal interacting with ammonia
(Ni, Zn, Co, Cu)
Tcarb=[550 - 700] °C
Component | % dipping solution
Bohemite | 0
Novolac 30 | 11
Formaldehyde | 2.4
Ethylenediamine | 0.4
Ni nitrate | 0.15

## Slide 6
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Experimental methods
Gas permeation tests
Pore size distribution
Laser microscope

## Slide 7
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Experimental methods
Gas permeation tests
Pore size distribution
Laser microscope
Separation performance
Single gas test
Mixed gas test

## Slide 8
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Experimental methods
*A. Rahimalimamaghani et al., ‘’ Effect of aluminium acetyl acetonate on the hydrogen and nitrogen permeation of carbon molecular sieves membranes’’, In.J of Hydrogen Energy (2022)
Kelvin equation
- - - -
*
Gas permeation tests
Pore size distribution
Laser microscope

## Slide 9
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Experimental methods
Gas permeation tests
Pore size distribution
Laser microscope
Quality of surface:
Surface roughness
Uniformity
Existence of cracks
3D Laser Confocal Microscope
Ra Ave. [µm] | Arithmetic average of profile height deviations from the mean line
Rz Ave. [µm] | Maximum peak to valley height of the profile

## Slide 10
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Results and discussion
Membrane performance separation with respect to Tcarb
AD dominant
AD dominant
MS dominant

## Slide 11
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Results and discussion
NH3 ~ He < H2
Kinetic diameter
Interaction between pore walls and NH3-H2
Pre-treatment with NH3, to investigate interaction with active sites
Mixed gas test
Mixed gas test
Single gas test
Membrane performance separation with respect to Tcarb

## Slide 12
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Results and discussion
Pore size distribution with respect to Tcarb
Limitation of the permporometry
Use of N2 as inert gas for the analysis
CM550 > CM700
pore size
From gas permeation test CM700 results to be more selective than CM550
CM700 narrow pores with highest pore percentage at 0.4 and 0.6 nm

## Slide 13
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Results and discussion
Surface characterization with respect to Tcarb
CM550
CM700
Ra [µm] | 0.119
Rz [µm] | 0.589
defects
Ra [µm] | 6.405
Rz [µm] | 70.730

## Slide 14
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)
3
N
H
H
H
Conclusions
NH3 and H2 chemical interaction with membrane walls
Higher carbonization temperature leads to have higher NH3 and H2 permeance compared to He
Main transport mechanism for NH3 is adsorption diffusion
Narrow pore size distribution for CM700 leads to have higher NH3/H2 and NH3/He selectivities

## Slide 15: Thank you for the attention! Questions??
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under grant agreement No 101058565 (Ambher project).
Funded by the European Union. Views and opinions expressed are however those of the author(s) only and do not necessarily reflect those of the European Union. Neither the European Union nor the granting authority can be held responsible for them
IX Symposium on Hydrogen, Fuel cells and Advanced Batteries, June 30-July 03, 2024, Milazzo (Italy)